American University of Beirut

Faculty of Engineering and architecture

Mechanical Engineering Department

Course: MECH 341

Report: Tensile Testing for Metallic Material (Lab 2)

Section: 2 (group 4)

Due Date: 7/3/2007

Instructor: Ali Ammouri

- Objectives:

Study the behavior of high carbon steel under tensile forces in order to determine the yield point, the ultimate tensile strength, and the failure point.

- Problem Approach:

We took a dog bone shaped high carbon steel specimen and subjected it to axial tensile forces using the Universal Testing Machine (UTM). The specimen is placed vertically between the two ends of the UTM in such a way the axis of the test specimen coincides with center lines of the heads of the testing machine. Moreover the extensometer gave the required data (Force and elongation) to study the elongation, the yield stress, the fracture load, the modulus of elasticity…

- Analysis and calculations:

The following properties were derived from a load-deflection:

- Yield Point Stress:

σ y = F/A0  = 50848/(πr2) = 50848/(π4.52 mm2)

= 799.6854MPa.

- Proportional Limit Stress:

σpl = F/A0 = 40082/(πr2) = 55200/(π4.52 mm2)

= 630.368MPa.

- 0.2% Offset Yield Stress:

σ0.2%y =579.755Mpa

- Ultimate Tensile Strength:

σult = Fult/A0  = 53300/(πr2) = 53300/(π*4.52 mm2)

= 837.8231 MPa.

- Engineering Fracture Stress = Fracture load/original area

= 52767/(π*4.52 mm2)

= 829.44 MPa

- True Stress :

σT = F/A = σ(1+ε)

- True Fracture Stress = Ffr/Ai =52767/61.645=855.98Mpa

Or another way,

=stress*(1+strain at fracture)

=855.983255*(1+0.031537426)=882.9787

- True Strain = εT = ln(1+ε). See the table.

- Percent Elongation of L “Gage Length” = 0.801/25*100

=3.204%

- Elasticity: using linear regression(taking different points on the linear part of the stress strain diagram) we get

E=slope of initial linear part of the stress strain curve

=468.654GPa

- Modulus of resilience

Ur= σy2/2E=0.8531Mpa

- Modulus of Toughness:

area under entire stress-strain curve:

Dividing the area under stress-strain curve into trapezoidal areas and summing them up we get:

Ut =24.62876Mpa

- Energy at yield=b*h/2

= 40082*0.099/2=1984.059.

- Energy at break: area under entire load deformation curve:

E=39172.04J

- Percent elongation=Lf-L0/L0*100=3.204%

- Percent reduction in area=(Afo-Ago)/Ago*100

= (63.617-61.645)/63.617 * 100

=3.1%

Afo= F/σT = 52767/855.9833=61.645mm2

4.Observations:

The specimen is stretched at a constant rate by the UTM. After a while, the specimen breaks producing a high breaking sound. The modulus of elasticity of this material is found to be 468.654GPa.

We did not observe necking in the specimen (the change in area is very small also in calculations 3.1%)

5. Conclusion:

From the stress-strain curve we notice that the larger part of the curve goes upward sloping until it breaks which shows that there was little plastic deformation. So we conclude that the material is brittle.

| Low carbon steel | High carbon steel |
| --- | --- |
| Necking then fracture. | Sudden fracture. |
| After fracture one end was concave and the other was convex. | Propagation of crack lines from a breakpoint. Surface of fracture is flat and rough. |
| Large plastic part. | Small plastic part. |

6. Appendix:

a) Force elongation

| Elongation(mm) | Force(N) |
| --- | --- |
| 0 | 53 |
| 0.001 | 640 |
| 0.003 | 7249 |
| 0.03 | 21213 |
| 0.077 | 35285 |
| 0.131 | 45518 |
| 0.278 | 52341 |
| 0.425 | 53140 |
| 0.558 | 53300 |

b) Stress-strain:

| strain | stress |
| --- | --- |
| 0.00012 | 113.94 |
| 0.001 | 308.2993 |
| 0.1544 | 834.4389 |
| 0.02148 | 837.7869 |
| 0.03204 | 829.409 |

c) True Stress strain

| True strain | True stress |
| --- | --- |
| 0 | 0.833071 |
| 4E-05 | 10.06013 |
| 0.00247 | 474.5314 |
| 0.004032 | 646.0134 |
| 0.008048 | 805.7034 |
| 0.031537 | 855.9833 |

d) This graph is used to calculate 0.2% -Offset Yield Stress: