AMERICAN UNIVERSITY OF BEIRUT

MECHANICAL ENGINEERING DEPARTMENT

SUBJECT: MECH 341

REPORT: # 3

Section 1

DUE DATE : 04/11/2009

- Objectives:

The main objective of this experiment was to:

- Measure and calculate the Brinell hardness of 5 different specimens (with different percentages of carbon), where hardness is defined as the resistance of an element to indentation.

2)  To determine the tensile strength (TS).

- Introduction:

3 different hardness tests are available:

a) Rockwell hardness test, indenter includes (spherical hardened steel balls and conical diamonds.

b) Brinell hardness test uses a hardened spherical ball as indenter.

c) Knoop and Vickers micro hardness test uses a small pyramidal shaped indenter.

However in our 3rd lab experiment we performed a Brinell hardness test. We have used a Brinell ball: the ball that transmits the indenting force is 10.000 mm in diameter. It is to be made of Tungsten Carbide and to be free of surface defects.

- Problem Approach:

Apparatus Settings:

•	Brinell Testing machine: consists of a test bed able to support the specimen and apply the indenting force to it via the indenter ball. The machine allows only vertical motion of the ball to avoid rocking and lateral sliding of the ball on the test specimen. The force applied is 500 Kg, 1500 Kg, or 3000 Kg according on the material to be tested. However, in this experiment we only used the 3 ton force( and every specimen was put under the action of that 3 ton force for about 30 sec)

•	Brinell ball: the ball that transmits the indenting force is 10.000 mm in diameter. It is to be made of Tungsten Carbide and to be free of surface defects.

•		Measuring device: used to measure the diameter of the indentation.

Test specimen:

There is no standard shape or size for a Brinell test specimen. The test specimen, however, must be thick enough not to bulge under the load (no signs of the load must appear on the opposite side). The test specimen is to be polished and cleaned to ensure accurate reading of the diameter.

The Brinell hardness test was performed on five types of specimens:

- Cast iron

- Low carbon steel specimen

- High carbon specimen

- Heat treated carbon steel specimen

- Brass

Preparation procedure for the heat treated Carbon steel specimen:

-Heat up specimen (in oven) to a temperature of 600oC (Time = 1hr)

-Raise temperature to 800oC in 10 minutes

-Keep specimen at 800oC for 25 minutes

-Quench specimen in oil at a temperature of 30oC

Procedure and measurements:

- set the required load on top of the machine (the 3000 kg load in this case)

- place the specimen on the flat surface below the Brinell ball

- apply the load on the specimen for about 30 sec

- Remove the specimen and measure the indentation diameter (d) using the microscope (two readings are taken at right angle and their average is to be used to determine the hardness of material).

- After finding the indentation diameter 2 methods are used to find the hardness either through tables or through the following formula:

- Analysis and calculations:

| Specimen | measure1 (d1 mm) | measure2 (d2 mm) | Average (mm) | Calculated HBW | Table Value for HBW | % error | TS (MPa) | % of carbon |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1- Cast iron | 4.4 | 4.3 | 4.35 | 191.811 | 192 | 0.098 | 560.8 | 0.32 |
| 2- Low carbon steel | 4.4 | 4.3 | 4.35 | 191.811 | 192 | 0.098 | 662.4 | 0.43 |
| 3- High carbon steel | 4.15 | 4.2 | 4.175 | 209.132 | 206.583 | 1.234 | 712.7114 | 0.55 |
| 4- Heat treated carbon steel | 2.8 | 2.7 | 2.75 | 495.349 | 495 | 0.070 | 1707.75 | -- |
| 5- Brass | 4.2 | 4.3 | 4.25 | 201.447 | 202 | 0.274 | 650.4 | 0.42 |

- We read tensile strength of the cast iron from graph (1) in the Appendix.

By knowing the HBW values which we found from the table, we can make a projection on the graph to get the value of the Tensile Strength.

- We calculated tensile strength of steels from the formula:

Tensile strength (MPa)=3.45*HBW.

- We calculated the percentage of carbon from graph (2) in the Appendix. By knowing the HBW values which we found from the table, we can make a projection on the graph with the fine pearlite curve to get the value of the carbon content (% of carbon).

- We calculated HBW:

- Note:

The HBW value for heat treated carbon steel for diameter of indentation : 2.75mm is not found in the chart, so we took an approximate value to the calculated value of HBW.

Analysis:

The presence of carbon makes dislocation between atoms harder, thus increasing the hardness of the material makes it more brittle.

Oppositely, when carbon is less present, the atoms move more freely, thus reducing hardness of the material makes it more ductile.

- Specimen 1 and 2 had the highest indentation diameter (4.35mm), and the lowest hardness number (192)( specimens 1 and 2 corresponds to casting iron and low carbon steel, where layers of ferrite and cementite are formed, consequently weakening the material.

- On the other hand, specimen 4 had the lowest indentation diameter (2.75mm), and the highest hardness number ( so, it experiences less plastic deformation. And as the percent of carbon increases the hardness of material increase. After quenching, the layers of materials will cool down rapidly, and this will transform the distribution of carbon from heterogeneous (dark layers including high concentration of carbon and light layers including low concentration of carbon) into homogenous structure, thus making the material harder because carbon atoms will redistribute evenly in the material.

- Specimen 4 corresponds to heat treated steel that has the highest percent composition of carbon between the 5 tested specimens. Upon heating, due to internal stresses the FCC crystal structure of steel will be altered into BCC structure.

- The high carbon steel specimen should have a higher hardness number that the low carbon steel specimen( specimen 3 is the high carbon steel. The high carbon steel has the same structure of low carbon steel, but a higher percentage of carbon.

- Cast iron is approximately has the same hardness as low carbon steel but has a lower hardness than high carbon steel, heat treated steel and brass.. It has a high percentage of carbon, but the impurities present in its structure weaken the material.

- Brass is much harder than cast iron and low carbon steel but has a lower hardness than high carbon and heat treated carbon steels. It also has a high percentage of iron but the impurities present in its structure weaken the material.

| Specimen1 | Specimen2 | Specimen3 | Specimen4 | Specimen5 |
| --- | --- | --- | --- | --- |
| Cast iron | Low carbon steel | High carbon steel | Heat treated carbon steel | Brass |

4. Observations:

Different indentations were observed for the different specimens. Thus, each specimen has hardness value different from the other.

5.Conclusion:

Every material has its own hardness, that is affected by its composition (especially the composition of carbon) and method of manufacturing (the heated treated steel was the hardest of the 5 specimens).

The ascending order of hardness of the 5 given specimens is as following: (low carbon steel and cast iron), brass, high carbon steel, heat treated carbon steel.

6.Appendix:

Graph 1:

Graph 2:

http://www.highpeaksteels.com/images/general/BRINELL%20HARDNESS%20TABLE%204.jpg